## Slide 1: Understanding “Position” in Welding
Walter J. Sperko, P. E.
Sperko Engineering Services, Inc.
4803 Archwood Dr.
Greensboro, NC 27406
www.sperkoengineering.com
sperko@asme.org
336-674-0600
FAX 336-674-0202

## Slide 2: This presentation posted on Sperkoengineering.com
The primary purpose of this presentation is twofold:
  Make sure that code users understand the difference between testing positions and production welding positions
  Help users understand how to read the figures that define production welding positions shown on the next page.

## Slide 3: Production Welding Positions
Groove Welds
Fillet Welds

## Slide 4: Standard Test Positions

## Slide 5: Standard Test Positions

## Slide 6: Standard Test Positions

## Slide 7: Standard Testing Positions
Test positions are discreetly defined positions of test coupons that are used when mostly when testing welders. These positions have tolerance of ±15° from the defined horizontal planes and ±5° from a defined vertical or inclined plane. See QW-120

## Slide 8: Testing Position 1G/PA
±15°
Weld Axis Horizontal
Plate Horizontal
±15°
Designations PA, PB, PD, etc. are the comparable
ISO 6947 equivalent posotioons

## Slide 9: Test Position 2G/PC
Plates Vertical
Weld Axis Horizontal
±15°
±15°

## Slide 10: Test Position 3F/PF or PG
±15°

## Slide 11: Test Position 6G/HL045 or JL045
45°± 5°

## Slide 12: Test Positions are Discreetly Defined
Because of tolerance limits on test positions, positions in between test positions are undefined!
That is, a weld that is inclined 22° uphill and rotated 36° about its axis has no “G” or “F” position. Such a position, however, may be encountered during production welding.
Production welding positions, therefore, need to be defined contiguously.

## Slide 13: Test Positions Qualify Welders for Specific Welding Positions
Test Positions  Welding Positions
Translations from test positions to welding positions are made in the construction codes. QW-461.9 is typical.

## Slide 14: Test Positions  Welding Positions

## Slide 15: Welding Positions
Note to table:
(1) Positions of welding as shown in QW-461.1 and QW-461.2
F = Flat
H = Horizontal
V = Vertical
O = Overhead
(2) Pipe 2-7/8 in outside diameter and over.

## Slide 16: Welding positions for groove welds are defined by the following diagram. NOTE Welding Position Diagrams are contiguous.

## Slide 17: Welding Positions for Groove Welds

## Slide 18: Tabulation showing transition points between welding positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizontal B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 19: Let’s start with the Flat Position

## Slide 20: Welding Positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizontal B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 21: Flat Positions Axis Inclination
15°

## Slide 22: Start at Nominal Flat Position
Face of weld is up

## Slide 23: Flat Upward Inclined Limit
15°
Weld may
incline upward
to a limit of 15°

## Slide 24: Flat Upward Inclined Limit
15°
But the welder
could be traveling
down the incline. . .

## Slide 25: Flat Downward Limit Is Implied
15°

## Slide 26: Welding Positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizonta B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 27: Flat Position --Rotation About Axis
180°
0°
30°
30°
150°
210°

## Slide 28: Flat Rolled Limit Clockwise
210°
180°
30°

## Slide 29: Flat Rolled Limit Clockwise
210°
180°
30°
Equivalent to
rotating
The plate 30°

## Slide 30: Flat Rolled Limit Counterclockwise
30°
150°
180°

## Slide 31: Flat Rotated Limits Not Considering Inclination
60°

## Slide 32: Welding Positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizonta B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 33: Flat Uphill Limit Rotated
15°
60°

## Slide 34: Flat Downhill Limit Rotated
15°

## Slide 35: Composite Flat Position Ranges
30°
60°

## Slide 36: Compare this range to 1G. . .

## Slide 37: Testing Position 1G/PA
±15°
Weld Axis Horizontal
Plate Horizontal
±15°

## Slide 38: Flat ≠ 1G !!!!

## Slide 39: Welding Positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizontal B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 40: Horizontal Position Axis Inclined
15°

## Slide 41: Basic Horizontal Position

## Slide 42: Horizontal Position Uphill Inclined Limit
15°

## Slide 43: Horizontal Position Downhill Inclined Limit
15°

## Slide 44: Welding Positions
Tabulation of Positions of Groove Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizontal B 0 to 15° 80 to 150°
210 to 280°
Overhead C 0 to 80° 0 to 80°
210 to 360°
Vertical D 15 to 80° 80 to 280°
E 80 to 90° 0 to 360°
How this table and the diagram on the previous page work are shown in the following diagrams

## Slide 45: Horizontal Position Rotated
80°
150°
70° range
210°
280°
70° Range

## Slide 46: Start at the Flat Rolled Limits
210°
180°
30°
Let’s go to an
end view. . . .

## Slide 47: Horizontal End View
30°
Horizontal starts where
Flat ends. . . .
210°

## Slide 48: Horizontal Rotates to where the plate is perpendicular to the ground
30°
Horizontal rotates
clockwise . .

## Slide 49: Horizontal Position Rotated Limit
30°
Horizontal ends
here. . . .
10°
90°
280°

## Slide 50: Non-inclined Horizontal Position Limits
70°
Starts with plate
Rotated 30°

## Slide 51: Non-inclined Horizontal Position Limits
70°
Finishes with plate
Rotated 10° beyond
perpendicular

## Slide 52: Composite Horizontal Position Limits
15°
15°

## Slide 53: Compare Horizontal to 2G

## Slide 54: Test Position 2G/PC
Plates Vertical
Weld Axis Horizontal
±15°
±15°

## Slide 55: Horizontal ≠ 2G!!!!

## Slide 56: Overhead Position
80°
280°
160° range

## Slide 57: Basic Overhead
Face of weld
is overhead!!!
0°

## Slide 58: Basic Overhead End View
Face of weld
is overhead
0°

## Slide 59: Overhead Partial Rotation End View
Face of weld
is overhead
0°

## Slide 60: Overhead Maximum Rotation End View
0°
280°
Face of weld on
This side

## Slide 61: Overhead Maximum Opposite Rotation End View
0°
280°
80°
Face of weld on
This side

## Slide 62: Same Rotation in Isometric View

## Slide 63: Basic Overhead
Face of weld
is overhead
0°

## Slide 64: Overhead Partial Rotation Isometric View
Face of weld
is overhead
0°

## Slide 65: Overhead Maximum Rotation Isometric View
0°
280°
Face of weld
On this side

## Slide 66: Overhead Maximum Opposite Rotation Isometric View
0°
280°
80°
Face of weld
is on this side

## Slide 67: Overhead Position Axis Inclination
80°
280°
160° range
80° range

## Slide 68: Basic Overhead for Inclined Axis
Face of weld
is overhead
0°

## Slide 69: Overhead Inclined Axis Rotation
0°
0°

## Slide 70: Overhead Inclined Axis Limit
0°
80°

## Slide 71: Overhead Inclined Axis Limit
0°
80°
Weld can rotate 360°
about vertical axis
while inclined 10°
forward tilt.

## Slide 72: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 73: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 74: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 75: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 76: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 77: Overhead Inclined Axis Limit
0°
Weld can rotate about
The vertical axis
10°

## Slide 78: Overhead Inclined Axis Limit
0°
Weld ends up back
Where it started!
10°

## Slide 79: Composite Overhead Position Limits
280°
80°
0°
0°
80°
360°
10°

## Slide 80: Overhead ≠ 4G !!!!

## Slide 81: Vertical Position Part 1
65° Range of Inclination
From 15 to 80°.
Face of weld is up
15°
80°

## Slide 82: Vertical Position Part 1
Range of inclination
Starts at 15°
Face of weld is up
15°

## Slide 83: Vertical Position Part 1
Range of inclination
continues upward. . .
Greater than 15°

## Slide 84: Vertical Position Part 1
Until reaching 80°
80°

## Slide 85: Vertical Position Part 2
When the “E” portion
of the
diagram is reached
80°

## Slide 86: Vertical Position Part 2
The “E” portion
of the diagram --
360° Rotation
About vertical axis
80°

## Slide 87: Vertical Position Part 2
The “E” portion of the
diagram begins here. .
80°

## Slide 88: Vertical Position Part 2
Partial rotation about
Vertical axis

## Slide 89: Vertical Position Part 2
More rotation about
Vertical axis

## Slide 90: Vertical Position Part 2
Even more rotation about
Vertical axis

## Slide 91: Vertical Position Part 2
Rotated 180° about
Vertical axis

## Slide 92: Vertical Position Part 2
Continuing Rotation about
Vertical axis

## Slide 93: Vertical Position Part 2
Continuing Rotation about
Vertical axis

## Slide 94: Vertical Position Part 2
Continuing Rotation about
Vertical axis

## Slide 95: Vertical Position Part 2
360° of Rotation about
Vertical axis completed

## Slide 96: Vertical Position Part 3
80°
280°
200° Range
of Rotation

## Slide 97: Vertical Position Part 3
Start here with inclination
Uphill or Downhill 15°
Face of weld upward
15°

## Slide 98: Vertical Position Part 3
Rotate face while holding
Inclination constant
15°

## Slide 99: Vertical Position Part 3
Continue rotating with
Inclination constant
15°

## Slide 100: Vertical Position Part 3
Rotated to vertical limit
Inclination constant
15°
280°

## Slide 101: Vertical Position Part 3
Return to starting position
Uphill or Downhill 15°
Face of weld upward
15°

## Slide 102: Vertical Position Part 3
Rotate face of weld
Opposite direction
Inclination Constant 15°
15°

## Slide 103: Vertical Position Part 3
Continue rotating
Opposite direction
Inclination Constant 15°
15°

## Slide 104: Vertical Position Part 3
Plate near vertical
Inclination Constant 15°
15°

## Slide 105: Vertical Position Part 3
Plate at vertical limit
of rotation.
Inclination Constant 15°
15°
80°

## Slide 106: Vertical Position Part 3
80°
280°
200° Range of
Rotation inclined
Uphill or Downhill 15°
15°

## Slide 107: Vertical Position Part 3
80°
280°
200° Range of Rotation
Inclination angle
Increases

## Slide 108: Vertical Position Part 3
280°
200° Range of Rotation
Inclination angle
Increases more. . .
80°

## Slide 109: Vertical Position Composite
80°
280°
160° range
65°
200°
360°

## Slide 110: Welding Positions for Fillet Welds

## Slide 111: Flat Fillet Weld

## Slide 112: Horizontal Fillet Weld

## Slide 113: Welding Positions for Fillet Welds

## Slide 114: Welding Positions for Fillet Welds
Tabulation of Positions of Fillet Welds
Position Diagram Reference Inclination of Axis Rotation of Face
Flat A 0 to 15° 150 to 210°
Horizontal B 0 to 15° 125 t0 150°
210 to 235°
Overhead C 0 to 80° 0 to125°
235 to 360°
Vertical D 15 to 80° 125 to 235°
E 80 to 90° 0 to 360°

## Slide 115: Welding Positions for Fillet Welds
The Horizontal Range
Is smaller for fillet welds
Than it is for groove welds

## Slide 116: Welding Positions for Groove Welds